## Slide 1: OBIGBO WIP ANALYSIS REPORT DRAFT
Date: 26th April, 2017
Authors: Jimmai Umaru, Onuigbo-Nweze Chy (SPDC)
Priye Lawson (NALCO)

## Slide 2: RESULTS (PH, TSS & TOTAL IRON)
S/n | Parameters | Method | Specification (Ops Manual) | Results (18-04-17) |  |  |  |  | Remarks
 |  |  |  | Source Well 21T | LP Discharge | Pump Discharge | D/S CUNO Filter (A) Injector well 22T | D/S CUNO Filter (B) Injector well 22T | 
1 | pH | API- RP45 | 5.5-6.5 | 6.19 | 6.38 | 6.28 | 6.01 | 6.18 | 
2 | TSS (mg/l) | ASTM- D5907 | <1 | 0.051 | 0.028 | 0.050 | 0.001 | 0.01 | 
3 | Total Iron (mg/l) | HACH | <5 | 6.34 | 5.84 | 6.69 | 6.65 | 6.10 | High Fe count likely due to corrosion, can be monitored as CI starts.
S/n | Parameters | Method | Specification (Ops Manual) | Results (20-04-17) | Remarks
 |  |  |  | D/S CUNO Filter (C) Injector well 22T | 
1 | TSS | HACH | <1 | 0.9 | 
2 | Total Iron | HACH | <5 | 6.55 | 

## Slide 3: RESULTS (DISSOLVED GASES)
S/n | Parameters | Method | Specification (Ops Manual) | Results |  |  |  |  | Remarks
 |  |  |  | Source Well 21T | LP Discharge | Pump Discharge | D/S CUNO Filter (A) Injector well 22T | D/S CUNO Filter (B) Injector well 22T | 
1 | Dissolved Oxygen (ppb) | HACH | <5 | 2000 | 7000 | 2000 | 1000 | 1000 | Mitigation: use of Oxygen scavenger & CI (to discuss with MCI team)
2 | Hydrogen Sulphide (ppm) | HACH | <1 | 0 | 0 | 0.1 | 0.3 | 0.25 | 
3 | Carbon Dioxide | HACH | NA?? | 40 | 40 | 45 | 45 | 45 | To confirm Specification from MCI

## Slide 4: RESULTS (TOTAL BACTERIA)
S/n | Parameters | Method | Results |  |  |  |  | Remarks
 |  |  | Source Well 21T | LP Discharge | Pump Discharge | D/S CUNO Filter (A) Injector well 22T | D/S CUNO Filter (B) Injector well 22T | 
1. | Total Bacteria M.E/ml( cATP) | Accucount | 1.39E+03 | 1.72E+03 | 4.09E+02 | 6.17E+04 | 1.13E+04 | Awaiting SRB results
< 1* 105 = Good Control
1* 105 - 1* 106 = Preventive Action
> 1* 106 = Corrective Action
NB: SRB result will be available 19th May, 2017.